Hydrogen peroxide and free available chlorine activation and quenching at non-ferrous/ic and non-cuprous/ic metal(loid) oxide surfaces: Potential applications for water treatment and beyond

Sin-Yi Liou1,2, Chu-Ching Lin1,3, Michael C. Dodd1*

# (1University of Washington, Seattle, WA, USA; 2Gwangju Institute of Science and Technology, Gwangju, South Korea; 3National Central University, Taoyuan City, Taiwan)

Presenting Author: Michael C. Dodd

# Keywords: Zirconium oxide, cerium oxide, reactive oxygen species, reactive chlorine species, oxidation, disinfection

# Introduction

Hydrogen peroxide (H2O2) and free available chlorine (FAC) are widely used in water and wastewater treatment as oxidants in their own right, or as sources of more reactive oxidants such as hydroxyl radical (HO•), chlorine radical (Cl•), chlorine monoxide radical (ClO•), or dichloride radical (Cl2•–) in advanced oxidation and disinfection processes. Conventional approaches for the "activation" of H2O2 or FAC to more reactive oxygen species (ROS) or reactive chlorine species (RCS) typically rely on UV photolysis or reactions with transition metals such as Fe2+/Fe3+ and Cu+/Cu2+ (e.g., in Fenton- and Fenton-like systems).

As potential non-photochemical alternatives to these more conventional approaches, we have investigated the use of non-ferrous/ic and non-cuprous/ic metal(loid) oxide (MeOx) phases including crystalline/monoclinic (m-ZrO2) and amorphous zirconium oxide (a-ZrO2), cerium oxide (CeO2), titanium oxide (TiO2), silicon oxide (SiO2), and aluminum oxide (Al2O3) as heterogenous catalysts for the dark activation of H2O2 and FAC in aqueous suspensions and pre-coat filtration systems. As a directly related aim, we have also evaluated the potential use of each MeOx for quenching residual H2O2 and FAC concentrations; for example, for H2O2 removal following UV/H2O2 AOPs, and for FAC removal from tap water by consumers at point-of-use. With these broader aims in mind, primary goals of this work were to evaluate (i) kinetics of H2O2 and FAC decomposition, (ii) associated generation of ROS and RCS, and (iii) degradation and inactivation of model organic compounds and microorganisms during reactions of H2O2 and FAC with each MeOx.

# Materials and Methods

All MeOx solids and other reagents were obtained from commercial sources, with the exception of a-ZrO2, which was synthesized from zirconium dichloride oxide octahydrate (ZrOCl2•8H2O) according to previously reported methods.1 Working H2O2 and FAC solutions were prepared from 30% w/w H2O2 and 4-5% w/w NaOCl. MeOx solids were characterized for particle size, specific surface area, pore volumes, and points of zero charge using appropriate analytical approaches. ROS and RCS identification and quantification were undertaken through the use of selective scavengers and probe compounds including tert-butanol, isopropanol, and methanol (for distinction amongst HO• and various RCS), furfuryl alcohol (for 1O2), tetranitromethane and nitro blue tetrazolium (for O2•–), as well as the use of D2O in place of H2O (for 1O2).

Experiments were typically undertaken by adding H2O2 or FAC to continuously-stirred suspensions of a given MeOx in 20-mL amber vials, at H2O2 or FAC concentrations of 0.1-100 mM and MeOx concentrations of 0.001-0.1 g/mL. Suspensions were also variously dosed with scavengers or probe compounds for characterizing the roles of ROS and RCS species in such systems. At pre-defined time intervals, samples were collected, filtered through 0.2-μm polyethersulfone (PES) syringe filters, analyzed for residual H2O2 or FAC, quenched with catalase or sodium thiosulfate to remove residual H2O2 or FAC, and subsequently analyzed by HPLC or other analytical methods as appropriate. For microbial inactivation experiments, MS2 bacteriophage (ATCC15597-B1) or Bacillus subtilis (ATCC 6633/BGSC 2A13) endospores were added to suspensions of selected MeOx in the presence of either H2O2 or FAC using similar approaches as above, except that samples were either plated directly on nutrient agar for B. subtilis endospore culturing or centrifuged prior to plating of the supernatant to a lawn of Escherichia coli C3000 (ATCC 15597) for MS2 plaque assays. Controls were undertaken in either the absence of oxidants or MeOx species.

# Results and Discussion

Under the batch treatment conditions investigated, H2O2 and FAC decomposition kinetics in the presence of each MeOx followed the order of a-ZrO2 > CeO2 > m-ZrO2 > Al2O3 > SiO2 > TiO2 for H2O2 and a-ZrO2 > CeO2 > Al2O3 > m-ZrO2 > SiO2 > TiO2 for FAC, with half-lives of oxidant decomposition ranging from <20 min for H2O2 and FAC decomposition by a-ZrO2 and CeO2 to more than 1 hr for H2O2 and FAC decomposition by m-ZrO2, Al2O3, SiO2, and TiO2. Selective scavenging and probe compound experiments indicated that decomposition of H2O2 and FAC on a-ZrO2, m-ZrO2, and CeO2 was accompanied by generation of substantial levels of 1O2 and/or O2•–, and lower levels of HO•. FAC decomposition on the same phases, as well as TiO2, also appeared to be accompanied by generation of RCS, potentially including Cl2•– and ClO•, though the identities of the specific RCS generated remain to be confirmed. Further experiments aimed at assessing potential use of these reactions in precoat filtration applications confirmed the degradation of furfuryl alcohol (1O2 probe) in H2O2- or FAC-containing solutions when passed continuously through thin layers of MeOx solids applied to 0.2-μm polyethersulfone (PES) at various flow rates.

Additional disinfection experiments demonstrated small apparent enhancements in the kinetics of B. subtilis endospore inactivation during exposure to FAC in the presence of CeO2 or TiO2 – presumably due to enhanced degradation of endospore coats by HO• and/or Cl•, and dramatic enhancements of MS2 bacteriophage inactivation during exposure to H2O2 in the presence of m-ZrO2 and CeO2 – presumably due to direct inactivation by the relatively high levels of 1O2 generated via catalytic decomposition of H2O2 in these systems. MS2 was also found to adsorb rapidly and completely to a-ZrO2 in the absence of H2O2, pointing to the potential use of this MeOx solid as an adsorbent material.

# Conclusions

On account of the apparent preferential generation of more-selective/weaker oxidants (e.g., 1O2, O2•–, ClO•) in favor of less-selected/stronger oxidants (e.g., HO•, Cl•), the catalytic decomposition of H2O2 and FAC on various MeOx surfaces processes appear to be most promising as targeted means of oxidation (e.g., pre-oxidation of dissolved organic matter for DBP mitigation, selective oxidation of easily-oxidizable substrates such as phenol- or aromatic amine-containing compounds) or disinfection (especially of viruses), versus more general advanced oxidation applications. Of the investigated oxidant+MeOx combinations, H2O2+a-ZrO2, H2O2+m-ZrO2, H2O2+CeO2, FAC+m-ZrO2, and FAC+CeO2 appear to be most promising for oxidation and disinfection applications. Additionally, a-ZrO2 and CeO2 appear to be particularly promising as options for rapid, catalytic quenching of excess H2O2 and FAC residuals following AOPs or at point-of-use.

# References

1.	Sobanska, K.; Pietrzyk, P.; Sojka, Z. Generation of reactive oxygen species via electroprotic interaction of H2O2 with ZrO2 gel: ionic sponge effect and pH-switchable peroxidase-and catalase-like activity. ACS Catalysis 2017, 7, 2935-2947.